## Slide 1: Automation of thermodynamic modeling
Alexander Richter, Shuang Lin
Oct 29th 2026

## Slide 2: Codes on github
Github website:
https://github.com/PhasesResearchLab/MatSE580GuestLectures

## Slide 3: Automation workflow
Motivation and background
Certain areas of parameterization and refinement procedure remain manual
Improve efficiency and reliability of CALPHAD modeling process
Open-source computational tools and our uniqueness​
PySIPFENN: Python package allows efficient predictions of the formation energy of atomic configurations
DFTTK: High-throughput first-principles calculations Tool Kit​
PyCalphad: Python library for computational thermodynamics using the CALPHAD
ESPEI: High-throughput modeling tool for ​creating CALPHAD databases
Application and Demo
Applying in building 9 refractory elements thermodynamic database (Cr-Hf-Mo-Nb-Ta-Ti-V-W-Zr)
Demo with Hf-Mo system

## Slide 4: ESPEI Overview
ESPEI, or Extensible Self-optimizing Phase Equilibria Infrastructure, is a tool for creating CALPHAD databases and evaluating the uncertainty of CALPHAD models.
What does ESPEI do?
  Parameter generation: generate model parameters for CALPHAD models of the Gibbs energy
  Optimization and uncertainty quantification: optimize and quantify the uncertainty of CALPHAD model parameters to thermochemical and phase boundary data
Reference: B. Bocklund et al., MRS Communications 9(2) (2019) 1–10. doi:10.1557/mrc.2019.59.
Websites: https://espei.org/en/latest/

## Slide 5: Phase name database
ESPEI-name.JSON
Provides the structure information:
Aliases_Name
Space_Group_Number
Strukturbericht_Designation
Prototype
Wyckoff_Positions
Comments
aflow_ID
Benefits:
Consistent phase names
Easy to add and update the phase information
Practice:
Try to find the phases information of your selected binary system

## Slide 6: LAVES phases of Hf-Mo
Phase name | Prototype | Pearson Symbol | Strukturbericht Designation | Space group (number) | Wyckoff Positions
LAVES_C15 | MgCu2 | cF24 | C15 | (227) | 8a,16d
LAVES_C14 | MgZn2 | hP12 | C14 | P63/mmc (194) | 2a,4f, 6h
LAVES_C36 | MgNi2 | hP24 | C36 | P63/mmc (194) | 4e,4f,4f,6g,6h
Phase name | Prototype | Pearson Symbol | Strukturbericht Designation | Space group (number) | Wyckoff Positions
LAVES_C15 | MgCu2 | cF24 | C15 |  | 8a,16d
LAVES_C14 | MgZn2 | hP12 | C14 | P63/mmc (194) | 2a,4f, 6h
LAVES_C36 | MgNi2 | hP24 | C36 | P63/mmc (194) | 4e,4f,4f,6g,6h
Mg atoms in red, Cu in blue, Zn in brown and Ni in light blue
C15
C14
C36

## Slide 7: Structures builder
Endmembers
  2n of each phase, where n is Wyckoff position
Dilute
  n*2n dilute POSCAR
  Near the most stable endmember
SQS
  BCC and HCP template
  SQS ATAT database
Phase name | Wyckoff Positions | Sublattice models
LAVES_C15 | 8a,16d | (Hf,Mo)1(Hf,Mo)2
LAVES_C14 | 2a,4f, 6h | (Hf,Mo)1(Hf,Mo)2(Hf,Mo)3
LAVES_C36 | 4e,4f,4f,6g,6h | (Hf,Mo)2(Hf,Mo)2(Hf,Mo)2(Hf,Mo)3(Hf,Mo)3
BCC_A2 | 2a | (Hf,Mo)1(VA)3
HCP_A3 | 2c | (Hf,Mo)1(VA)0.3
https://phaseslab.com/#/resources/

## Slide 8: Automation workflow
Motivation and background
Certain areas of parameterization and refinement procedure remain manual
Improve efficiency and reliability of CALPHAD modeling process
Open-source computational tools and our uniqueness​
PySIPFENN: Python package allows efficient predictions of the formation energy of atomic configurations
DFTTK: High-throughput first-principles calculations Tool Kit​
PyCalphad: Python library for computational thermodynamics using the CALPHAD
ESPEI: High-throughput modeling tool for ​creating CALPHAD databases
Application and Demo
Applying in building 9 refractory elements thermodynamic database (Cr-Hf-Mo-Nb-Ta-Ti-V-W-Zr)
Demo with Hf-Mo system

## Slide 9: ESPEI Input data
Phases and CALPHAD models

## Slide 10: ESPEI Input data
Non-equilibrium Thermochemical Data
  This can in principle be any thermodynamic quantity, but currently only CPM*, SM*, and HM* (where * is either nothing, _MIX or _FORM) are supported.
Equilibrium Thermochemical Data
  Activity data
  Enthalpy of formation data in region with two or more phases in equilibrium
  Enthalpy of formation for a phase with multiple sublattice, e.g. the σ phase

## Slide 11: ESPEI Input data
Phase Diagram data
ESPEI can consider multi-component phase diagram data with an arbitrary number of phases in equilibrium. Phase diagram data JSON datasets are distinguished by using "output": "ZPF”.
Each entry in the JSON values corresponds to a phase region where one or more phases are participating in equilibrium under the given temperature and pressure conditions.

## Slide 12: Hf-Mo phase boundary data
Webplotdigitizer get the experimental data in template
ZPF_to_JSON.py convert ZPF data to ESPEI readable JSON

## Slide 13: Units
Energies are in J/mol-atom (and the derivatives follow)
All compositions are mole fractions
Temperatures are in Kelvin
Pressures in Pascal

## Slide 14: Pysipfenn result to ESPEI JSON

## Slide 15: DFTTK Mongodb to espei JSON
Get the tags information from METADATAS after submitting DFTTK job
DFTTK_to_ESPEI_JSON.py
  Connect with dfttk MongoDB
  Target the systems with tags information
  Convert EOS fitting energy to formation enthalpy in ESPEI JSON format
Notes: Brando liquid the
Pop file for liquid

## Slide 16: Hf-Mo LAVES_C15
Sublattice model (Hf,Mo)1(Hf,Mo)2
2 dilute structures of the most stable endmembers
Lattice occupation | 
16 | 32
Hf 16 | Hf, Mo 1, 31
Hf, Mo 15, 1 | Mo 32

## Slide 17: Hf-Mo LAVES_C14
Lattice occupation |  | 
1 | 2 | 3
Hf 16 | Mo,Hf 7,1 | Mo 24
Hf 16 | Mo 8 | Mo,Hf 23,1
Hf,Mo 15,1 | Mo 8 | Mo 24
Sublattice model (Hf,Mo)2(Hf,Mo)1(Hf,Mo)3
3 dilute structures of the most stable endmembers

## Slide 18: Hf-Mo LAVES_C36
Lattice occupation |  |  |  | 
1 | 2 | 3 | 4 | 5
Hf 8 | Hf 8 | Mo,Hf 7,1 | Mo 12 | Mo 12
Hf 8 | Hf 8 | Mo 8 | Mo,Hf 11, 1 | Mo 12
Hf 8 | Hf 8 | Mo 8 | Mo 12 | Mo,Hf 11, 1
Hf,Mo 7,1 | Hf 8 | Mo 8 | Mo 12 | Mo 12
Hf 8 | Hf,Mo 7,1 | Mo 8 | Mo 12 | Mo 12
Sublattice model (Hf,Mo)2(Hf,Mo)2(Hf,Mo)2(Hf,Mo)3(Hf,Mo)3
5 dilute structures of the most stable endmembers

## Slide 19: Input data for ESPEI parameter selection
Visualize the HM surface of LAVES_36 phase in 2-D

## Slide 20: Phase diagram generation by ESEPI Parameter selection
First-principles + machine learning
Input data of Formation_H
BCC and HCP: 2 endmembers+ 3 SQS + 4 dilute
C15: 4 endmembers+ 4 dilute
C14: 6 endmembers + 6 dilute
C36: 32 endmembers+ 10 dilute
Liquid: No interaction parameter
66 parameters in the generated TDB

## Slide 21: ESPEI MCMC optimization
Posterior probability : p(θ|D), of the model parameters, θ, conditioned on the data, D
The prior: p(θ), contains the domain knowledge of the modeler in the probability distribution of each parameter.
The likelihood: p(D|θ), is the probability that the data are described by a set of parameters
The evidence : p(D), is the probability of the data marginalized over the possible parameters
Optimizing model parameters by Bayes theorem

## Slide 22: Phase diagram optimization by ESEPI MCMC
Convergence of the posterior log probabilities from the MCMC simulation.
Converge after 100 iterations.

## Slide 23: Run ESPEI MCMC on Roar collab
Activate environment in Roar collab
conda activate your ESPEI environment
Prepare the input data:
  Input files (json)
  MCMC setting.yaml
Sbatch job file:

## Slide 25: Thermodynamic modeling methodology
LAVES phases
Laves_C15 of HfMo system, sublattice model (Hf, Mo)2 (Hf, Mo)1, The Gibbs energy of a HfMo2 phase is generally formulated as:
Reference state energy :
Ideal mixing energy:
Interaction energy between different components in the same sublattice:
+